## Slide 1: Density Functional Theory and Machine Learning applied for Perovskite Materials
Jiri Hostas
8th Annual Alberta Nano Research Symposium
April 1, 2023
Funded by AI4D NRC project: Dennis Salahub, John Garcia, Hatef Shahmohamadi, Maicon Lourenco,
Alain Tchagang, Venkataraman Thangadurai, and Karthik Shankar
github.com/jiri-hostas

## Slide 2: Outline
Results
  1. Role of Vacancies and AL
  2. Experimental dataset
    Descriptors
    Regression models
    Visualization
Conclusions
Graphic for periodic table trends taken from DOI: 10.1039/C7NH00010C
A1 A2 B1 B2 A1/B1 A1*B1
Fe
Introduction
  Perovskite chemistry
  Where can ML help?

## Slide 3: Oxide Perovskites
CaTiO3, ABO3, or AA’BB’O6
Functional materials
Versatile catalysts:
  Water splitting reaction
  CO2 reduction
Semiconductors
Graphics for structural flexibility is from DOI 10.1039/c8ee01574k
Notes: Originally CaTiO3 but many other cations can be substituted: A and B are large electropositive cations. The ideal cubic structure has the B cation in 6-fold coordination, surrounded by an octahedron of anions, and the A cation in 12-fold cuboctahedral coordination

## Slide 4: Theoretical Studies
Coarse grain & Mesoscale
Molecules & Segments
Force Fields
Atoms
e.g. ReaxFF, UFF
Semi-empirical QM
Orbitals
DFTB
Ab initio
Electrons
DFT-D

## Slide 5: Accelerating Material Science Using AI/ML
2. Predict properties or
propose new materials
3. robotics/optimization
of reaction conditions
1. Material
structure and characterization
Graphics for autonomous chemical experiments taken from 10.1021/acs.accounts.2c00220

## Slide 6: 1. Role of Vacancies in CaTiO3
Maicon P. Lourenço, Lizandra Barrios Herrera, Jiří Hostaš et al. Phys. Chem. Chem. Phys. 2022, 24, 25227
Pristine CaTiO3
Modified CaTiO2.625
(B)
(A)
Active Learning
Notes: - low oxygen atmosphere ...

## Slide 7: Number of Double-Perovskites
AA’BB’O6
>> 107 combinations
Narrow bandgap is important for e.g. semiconductors
Catalysts for specific reactions have a certain bandgap range

## Slide 8: 2. ML for Direct Prediction of Band Gap
The Materials Database
Reflection of research focus and interests, method of measurement/calculation, dataset size, type of compounds etc.
Experiment

## Slide 10: 1st step: Composition only
training
testing
39 features, weight compositions:
['Bi', 'Ca', 'Fe', 'O', 'Gd', 'Cr', 'Sr', 'Ta', 'Ni', 'Mo', 'Li', 'Cu', 'Ba', 'Sc', 'W', 'Co', 'Nb', 'La', 'Mg', 'Mn', 'Eu', 'Dy', 'Lu', 'Ag', 'I', 'Na', 'Ti', 'Sm', 'Zn', 'Pr', 'V', 'Ce', 'Nd', 'In', 'Te', 'Ga', 'Tb', 'Y', 'Al']
Key takeaway:
slight improvement
when we optimize
the models but still a
weak descriptor
Bi1Ca1Fe2O6 double-perovskite weight composition vector:
[0.46, 0.09, 0.24, 0.21, 0.00, … ]
[ Bi, Ca, Fe, O, Gd, … ]
Notes: Default hyperparameter model versus hyperparameter optimized model.

## Slide 11
Descriptors included:
  Compound mass composition
  Sample preparation
  Atomic features (tabulated)
    Shannon’s ionic radii
    Ideal bond length
    Electronegativity
    Van der walls radius
    Ionization energy
    Molar volume
    Atomic number
    Atomic mass
  Geometric criteria
    Tolerance factor
    Octahedral factor
Target property:
  Experimental Bandgap
From literature
From periodic table
of elements
Bi1Ca1Fe1O3 double-perovskite weight composition vector (before std):
[0.46, 0.09, 0.24, 0.21, 0.00, … ]
[ Bi, Ca, Fe, O, Gd, … ]

## Slide 12
MSE: 0.02
MAE: 0.06
R2: 0.98
MSE: 0.35
MAE: 0.35
R2: 0.55
A1 A2 B1 B2
A1 A2 B1 B2 A1/B1 A1*B1
MSE: 0.02
MAE: 0.07
R2: 0.97
MSE: 0.30
MAE: 0.24
R2: 0.62
MSE: 0.04
MAE: 0.07
R2: 0.95
A1 A2 B1 B2 A1/B1 A1*B1 factors
Added geometrical factors
MSE: 0.32
MAE: 0.24
R2: 0.59

## Slide 13
Weight compositions descriptor
A1 A2 B1 B2 A1/B1 A1*B1
MSE: 0.02
MAE: 0.07
R2: 0.97
MSE: 0.30
MAE: 0.24
R2: 0.62
training
testing
overfitting

## Slide 14
Feature engineering/reduction and visualization
Principal Component Analysis
3D data
2D data
PC3
PC2
PC1

## Slide 15: PCA
A1,A2,B1,B2
A1/B1,A1B1
A2/B2,A2B2
A1,A2,B1,B2
A1/B1,A1B1
A1,A2,B1,B2

## Slide 16: Latent Space via Wasserstein Autoencoders
To reduce the high-dimensional search space
Data visualization
*Ziyuan Rao et al. Science 2022, 378, 78
Figure S4A: Deep generative model. “Although WAE is trained
only on compositional data, it may include information
on composition-related properties… making the latent
space physically meaningful and informative.”*
Notes: Constrained autoencoder architecture by Gaussian prior. Lrec is binary cross-entropy of input-output pair and Lreg is defined as maximum mean discrepancy (MMD) between the latent space distribution and a Gaussian prior. MMD is a kernel-based statistical measure used to determine whether given two distributions are the same. Two distributions are similar if their moments are similar.

## Slide 17: Wasserstein Autoencoders
64 features for
A1,A2,B1,B2
A1/B1,A1B1
A2/B2,A2B2

## Slide 18: Conclusions
ML to accelerate DFT
Tested different descriptors (weight and molar composition, elemental…)
Generate a latent space to visualize the dataset
We need to generate more data for successful ML applications (without overfiting)
(combine experimental and calculated data)
Results published in:
Maicon P. Lourenço, Lizandra Barrios Herrera, Jiří Hostaš Patrizia Calaminici, Andreas M Köster, Alain Tchagang, Dennis R Salahub, Phys. Chem. Chem. Phys. 2022, 24, 25227
Jiří Hostaš et. al Compositional and elemental descriptors for perovskite materials. In Workshop on ''Machine Learning for Materials'' ICLR 2023, 2023

## Slide 19: Acknowledgement
Dr. Dennis Salahub
Dr. Maicon Lourenço
Dr. Venkataraman Thangadurai
Dr. Karthik Shankar
Dr. Alain Tchagang
John Garcia
And all my colleagues and collaborators

## Slide 20
Thank you for your attention,
questions and comments!